## Slide 1
Mehdi Ghrabli, Mounira Bouarroudj, Ludovic Chamoin, Emanuel Aldea
mehdi.ghrabli1@ens-paris-saclay.fr
CNRS, SATIE & LMPS Laboratories
Hybrid modeling for remaining useful life prediction in power module prognosis
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
April 8, 2024

## Slide 2
1
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 3
2
GENERAL CONTEXT
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
INTRODUCTION
Exponential growth in electric cars market
Alternative for fossil fuel-powered vehicles
2035 zero-emission agreement
Electric car sales, 2016-2023 [1]

## Slide 4
3
PROBLEM
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
INTRODUCTION
Estimate the lifetime of electric modules
Classical answer : Point estimates
  Environmental temperature? (Warm/Cold)
  Frequency of usage? (Extreme/Moderate)
  Remaining useful life after degradation?
An empirical model for failure prediction [2]

## Slide 5
4
GENERAL PURPOSE
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
INTRODUCTION
Given a load profile + sequence of observed previous states, estimate the remaining useful life (RUL) of the power electronic module caused by damage in the wire bonds

## Slide 6
5
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 7
6
HEALTH INDICATOR
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DAMAGE MECHANISM
Monitor using non-intrusive measurements
Collector-emitter voltage : viable to assess degradation in the top interconnexions
Increase of 5% w.r.t. initial value = failure
Evolution of the relative variation of the collector-emitter voltage during test cycles [4]
Degradation in a bond wire [3]

## Slide 8
7
PARIS’ LAW
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DAMAGE MECHANISM
Experimental illustration of Paris’ law [5]
: Crack length
: Loading cycle
: Stress intensity factor variation
: Constants
Paris-Erdogan equation

## Slide 9
8
IRWIN’S EQUATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DAMAGE MECHANISM
Polar coordinate system near the crack tip [6]
: Component of the stress matrix
: Polar coordinates
: Known trigonometric function
Irwin’s equation

## Slide 10
9
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 11
10
EXPERIMENTAL DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
6 runs to failure showing evolution w.r.t.
≈ 95 data point per run
Runs to failure showing evolution w.r.t. [4]

## Slide 12
11
EXPERIMENTAL DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Destructive campaigns leading to 96 data points showing normalized variation with respect to (Left) and relative variations (Right) [4]

## Slide 13
12
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Full geometric model of the IGBT
Simplified geometric IGBT model

## Slide 14
13
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Geometric modeling of a crack of length
Reduce contact size according to a crack size

## Slide 15
14
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Geometric modeling of a crack of length
Reduce contact size according to a crack size
Apply current inducing self-heating identical to experiments

## Slide 16
15
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Geometric modeling of a crack of length
Reduce contact size according to a crack size
Apply current inducing self-heating identical to experiments
Measure

## Slide 17
16
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Geometric modeling of a crack of length
Reduce contact size according to a crack size
Apply current inducing self-heating identical to experiments
Measure
Calculate

## Slide 18
17
SIMULATED DATA
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
DATASETS
Geometric modeling of a crack of length
Reduce contact size according to a crack size
Apply current inducing self-heating identical to experiments
Measure
Calculate
Repeat for different values of

## Slide 19
18
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 20
19
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Estimate evolution of w.r.t. given previous observations
Iterative process
Governed by the Paris regime : ( )
Prediction framework.

## Slide 21
20
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime

## Slide 22
21
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Regression

## Slide 23
22
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Numerical simulation

## Slide 24
23
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Paris’ law

## Slide 25
24
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Adding to previous value

## Slide 26
25
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Using (inverse) regression

## Slide 27
26
FORMULATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Check :
In Paris regime
Not in Paris regime
Adaptive interpolation until failure/Paris regime

## Slide 28
27
INTERPOLATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Apply polynomial interpolation to training data
Find the optimal degree (minimizes residual error)
Degree 3 polynomials were used

## Slide 29
28
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
Degree 3 polynomials as an approximation of w.r.t.

## Slide 30
29
INTERPOLATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
METHODOLOGY
increment growth assumed to be polynomial of degree
Polynomial of degree is fitted on observed test increments
Generate increments using fitted polynomial
Degree 2 polynomial fitted on observed test increments

## Slide 31
30
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 32
31
PARIS’ LAW VALIDITY
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
50 simulated points relating to
Paris regime : linear regime on the log scale
Simulated data on the logarithmic scale
Logarithmic Paris equation

## Slide 33
32
PARIS’ LAW VALIDITY
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
Linear regression on Paris simulations

## Slide 34
33
VALIDATION PROCESS
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
5 runs to failure are used in training
Cross validation is used ( 6 folds)
Percentage of observed test values : 10%, 20%, 30%

## Slide 35
34
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
Predictions on 10% of observed test data

## Slide 36
35
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
Predictions on 20% of observed test data

## Slide 37
36
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
RESULTS
Predictions on 30% of observed test data

## Slide 38
37
Introduction
Damage mechanism
Datasets
Methodology
Results
Conclusion
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
OUTLINE

## Slide 39
38
KEY TAKEAWAYS
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
CONCLUSION
Paris’ law is viable to describe an important phase of the power module’s lifetime
Incorporating physical knowledge adaptively limits losses in accuracy due to incompleteness in said knowledge
Pairing data with physical models can achieve accurate and robust predictions in complex applications, with possibilities of extrapolation

## Slide 40
39
FUTURE WORK
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
CONCLUSION
Probabilistic predictions
Uncertainty incorporation
Extrapolation to unseen conditions
Gaussian process-based regression to estimate from

## Slide 41
40
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
REFERENCES
[1] IEA, Electric car sales, 2016-2023, IEA, Paris https://www.iea.org/data-and-statistics/charts/electric-car-sales-2016-2023, IEA. Licence: CC BY 4.0
[2] M. Held et al. "Fast power cycling test of IGBT modules in traction application," Proceedings of Second International Conference on Power Electronics and Drive Systems, 1997
[3] O. Schilling et al. Power cycling testing and fe modelling focussed on al wire bond fatigue in high power igbt modules. Microelectronics Reliability, 2012.
[4] N. Dornic. Elaboration et comparaison de deux modèles de durée de vie des fils d’interconnexion des modules de puissance, l’un base sur les déformations et l’autre sur les dégradations. PhD thesis, Université Paris-Saclay, 2019
[5] R. O. Ritchie. Near-threshold fatigue crack propagation in ultra-high strength steel: Influence of load ratio and cyclic strength. 1976
[6] F. Fremy. Fissuration par fatigue en mode mixte I+II+III non proportionnel dans l’acier 316L : approche expérimentale et modélisation des effets de la plasticité. PhD thesis, ENS, 2012

## Slide 42
41
REGRESSION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Crack length w.r.t. relative variation (Paris prediction)
Normalized crack length with respect to relative variation

## Slide 43
42
REGRESSION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Crack length w.r.t. current cycle (Calibration)
Normalized crack length with respect to normalized test cycle

## Slide 44
43
DATASET )
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
and two different simulations :
;

## Slide 45
44
ORDER INCREMENTS
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
A polynomial function of degree
: Polynomial function of degree

## Slide 46
45
INCREMENETS QUANTIZATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Parabolic behavior of increments w.r.t. cycles
Reduce the number of possible values of increments to possible values
Increment quantization on 50 bins

## Slide 47
46
INCREMENETS QUANTIZATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Quadratic decrease of the number of cycles per bin

## Slide 48
47
INCREMENETS QUANTIZATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Quadratic decrease of the number of cycles per bin illustrated by a square root growth of the inverse of the numbers of cycles per

## Slide 49
48
ADAPTIVE INTERPOLATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Quantization of a partially observed run
Quadratic decrease of the number of cycles per bin of a partially observed run

## Slide 50
49
ADAPTIVE INTERPOLATION
25th International Conference on Thermal, Mechanical and Multi-Physics Simulation and Experiments in Microelectronics and Microsystems
Catania, April 7-8-9-10, 2024
APPENDIX
Quadratic decrease of the number of cycles per bin of a partially observed run bin, illustrated by a square root growth of the inverse of the numbers of cycles per